## Slide 1
Sojiro Sugiura
Nagoya University
Engineering, 1st doctoral student
Intelligence robotics laboratory
Closed-Loop Physical Optimization
of Soft Sensorized Gloves
and High-Reproducible Sensor Print

## Slide 2: Problems and contributions
Problems:
Low reproducibility of the 3D print
High base-resistance and low viscosity lower sensor quality
Complex sensor morphology on thumb
Contributions:
Automatic print setup increased print reproducibility
Material that lowers baseline while enhances viscosity
Closed-loop optimization for finding better sensor shape
Keywords:
Soft sensor
3D print
Wearable glove
Optimization

## Slide 3: 5 bullets list
Goal:
Finding out complex morphology of soft sensor printed on glove to detect specific motion of hand
Problems:
Complex mechanism of thumb to detect hand motion accurately using printable soft sensor
Hypothesis:
Closed-loop optimization cycle will improve the sensitivity gradually, and quick & high-reproducible 3D print setup is needed
Proof:
Bayesian optimization found shape which is only sensitive for specific motion through 40 cycles. It turned out this process was personalization rather than general optimization.
Conclusion:
Closed-loop optimization of physical printable sensor can find better shape of sensor for specific purpose

## Slide 4: Index
1. Introduction
Overview of hydrogel and glove sensor → prblems and approach
2. Material
2.1. Automatic 3D print setup, 2.2. Hydrogel with Corn flour
3. Optimization method
3.1. Basic results, 3.2. Bayesian, 3.3. Parameters
4. Results & Discussion
5. Conclusion
1. Introduction
Overview of hydrogel and glove sensor → prblems and approach
2. 3D printer
2.1. Printer Setup, 2.2. Automatic Print Diagram
3. Hydrogel
3.1. Print Quality, 3.2. Electrical Property
4. Sensor shape
4.1. Basic shapes, 4.2. Optimization Process, 4.3. Results
5. Discussion
6. Conclusion

## Slide 5: Figures
Fig.1 Our proposed optimization cycle
Fig.2 Setup of the automatic 3D printer and print diagram.
Fig.3 Print quality & electric property of the hydrogel containing cornflour
Fig.4 Sensitivity according to the sensor shape. Repeatability
Fig.5 Optimization diagram and parameters
Fig.6 Gloves in the process of the optimization and results

## Slide 6: Figure1 Overview
Fig.1 Overview of this study
Output
Iteration

## Slide 7: Figure1 Overview
Fig.1 Overview of this study
Sensitivity
Iteration
Hand scan
3D printer
Print
Printed sensor
Measurement
Optimization

## Slide 8: Figure1 (Automatic 3D printer)
Fig.2 Setup of the automatic 3D printer: nozzle, camera, and print diagram.
Command type
Speed
X point
Y, Z point
Extrusion amount
Camera
640×480
Print plate
225×225
RGB-Stereo camera
Heated nozzle
& Hydrogel
① Make 2D model
② Generate print-code
Set target points
on print-plate
Set object
on the points
③
④
② Hand detection
(a) Manual setup of 3D print
Camera vision
3D printer
Camera information
Print command
Computer
3D printer
Camera
XY trajectory
planning
③
Height
measurement
④
① Sensor shape selection
Width
Pattern
Length
⑤ Coordinate transformation
⑥ Print code generation
⑦ Print start
a)
b)
c)

## Slide 9: Figure3 and Table1 Stability of sensor
Fig.3: Thin printed sensor shows high baseline resistance and dominant capacitance. Thick printed sensor has better electric properties, but its viscosity is too low to print accurate and complex shapes
① Thin sensor
② Thick sensor
③ Corn-flour sensor
Thickness: 4 mm
Base resistance: 80 MΩ
Phase shift: -30 - 15 deg
Base resistance
Thickness: 8 mm
Base resistance: 22 MΩ
Phase shift: 15 deg
Thickness: 2 mm
Base resistance: 25 MΩ
Phase shift: 13 deg
Try some materials (Normal, more salt, more gelatine, glaphene, cornflour)
Normal is low viscous, thixotropy is also low
Salt does not affect the viscosity, but improves the base resistance
Gelatine enhances its viscosity and thixotropy too much (Extrusion is difficult)
Cornflour enhances its viscosity and thixotropy well
Glaphene enhance its thixotropy, but not viscosity
 | Material | Thickness | Contact angle or height | Base resistance | Phase shift
1 | Normal hydrogel | 4 mm |  | 80 MΩ | -30 deg - 15 deg
2 | Normal hydrogel | 8 mm |  | 22 MΩ | 15 deg
3 | Salt 4 → 8%wt | 4 mm |  |  | 
4 | Gelatine 40 → 50%wt | 2 mm |  |  | 
4 | Gelatine 40 → 60%wt | 2 mm |  |  | 
5 | + Corn-flour 20%wt | 2 mm |  |  | 
6 | + Corn-flour 40%wt | 2 mm |  |  | 
7 | + Glaphene 10%wt | 2 mm |  |  | 
8 | + Glaphene 20%wt | 2 mm |  |  | 
Rapid viscosity increase ← Contact angle
Apporopriate viscosity ← Mesh test
Material electric property ← cast test
Target
Low base resistance (includes time scale effect)
Thin printed
Notes: Line thicker, Font, align

## Slide 10: Figure3-3 (Print quality)
Fig.3 Cornflour print: printability by the amount of cornflour.
No cornflour
Cornflour 40 wt%
Cornflour 20 wt%
Cornflour 60 wt%
Gelatine 60%wt
30 mm
Corn flour amount
Viscosity
(b) Mesh shape print process
(c) Mesh print results
Glaphene 10%wt
Fine print zone
Shear thinning
Continuous extrusion
Rapid viscosity increase
No delamination
Rapid viscosity increase ← Contact angle
Apporopriate viscosity ← Mesh test
Material electric property ← cast test
Temperature
Viscosity
30℃
35℃
40℃
45℃
Fine print zone
Corn 20%wt
35 ℃
Corn 40%wt
35 ℃
Corn 20%wt
45 ℃
Salt 8wt%
30 ℃
Original
40 ℃
Original
Salt 4%wt→8%wt
+ Corn flour 20%wt
+ Corn flour 40%wt
Original
30 ℃
(a) Fine print viscosity
Notes: 1) the polymers should be highly thixotropic and exhibit shear thinning behavior,
2) appropriate viscosity such that the material can be extrudable and form continuous filaments to ensure structure fidelity,
3) Undergoes a rapid viscosity increase after extrusion to retain the 3D printed shape,
4) sufficient mechanical strength after exiting the nozzle is required to support the subsequently printed structures and to prevent delamination during and after printing.

## Slide 11: Figure3-2 (Salt vs base resistance)
Fig.4-1 As the amount of salt increases, the baseline resistance decrease.
The influence by time was also examined.
Chart: Salt [wt%]
| 0 | 4 | 8 | 12 | 16 | 20
1hr | 1 | 0.10364 | 0.049091 | 0.036364 | 0.04 | 0.027273
24hr | 1 | 0.092334 | 0.032404 | 0.025087 | 0.028571 | 0.016028
48hr | 1 | 0.077922 | 0.024675 | 0.016883 | 0.018182 | 0.0092208
Average | 1 | 0.091298 | 0.03539 | 0.026111 | 0.028918 | 0.017507
Chart: Cornflour [wt%]
| 0 | 4 | 20 | 30 | 40 | 50
 | 1 | 0.72222 | 0.72222 | 1.2778 | 1.7778 | 3.2222
Being stickey
Stress -Strain
Strain-Resistance
(a)
(b)
(c)
(d)

## Slide 12: Figure4 (Simple sensor shape and sensitivity)
Fig.4 Sensitivity according to the sensor shape
Thickness
Base resistance
Middle
Full
Chart: Sensitivity
Day1 | 1.1827 | 1.1713 | 1.1948 | 1.1907 | 1.1899 | 1.2168
Day2 | 1.1836 | 1.1881 | 1.1725 | 1.1939 | 1.1749 | 1.1859
Thick
Thin
Chart: Resistance Change Ratio
| Simple-U | U-narrow | U-wide | W-short | W-middle | W-long | Sine
Middle | 1.1209 | 1.181 | 1.0765 | 1.1157 | 1.1497 | 1.1358 | 1.1205
Full | 1.1832 | 1.2322 | 1.1278 | 1.1438 | 1.1622 | 1.1717 | 1.1555
(a)
(b)
(c)
Notes: Font and line size

## Slide 13: Figure 5 Optimization diagram
Generating
print code
3D print
Measurement
Learning
the results
Bayesian
optimization
Deciding
next shape
Simulation
phase
Real-world
phase
Target
Motion
Optimized shape
Start
Complete
⑤ Width
② Start
④ Angle
① Offset
③ End
0°≦ θ ≦ 45°
θ
0
1
0.5
7 mm ≦ w ≦ 14 mm
w
Target motion 1
Pose 1
Pose 2
Pose 3
Target motion 2
Pose 4
Pose 5
Pose difference ratio
Control Input
Output

## Slide 14: Figure 5 Optimization diagram
Generating
print code
3D print
Measurement
Learning
the results
Bayesian
optimization
Deciding
next shape
Simulation
phase
Real-world
phase
Target
Motion
Optimized shape
Start
Complete
⑤ Width
② Start
④ Angle
① Offset
③ End
0°≦ θ ≦ 45°
θ
0
1
0.5
7 mm ≦ w ≦ 14 mm
w
Target motion 1
Pose 1
Pose 2
Pose 3
Target motion 2
Pose 4
Pose 5
Pose difference ratio
Control Input
Output

## Slide 15: Figure 6 Optimization results
1
2
3
43
44
45
Better
Worse
・・・

## Slide 16: Figure 6 Optimization results
Chart: Iteration
 | 1.0479 | 1.04 | 1.0915 | 1.0811 | 1.0131 | 1.062 | 1.0952 | 1.0776 | 1.0339 | 1.037 | 1.0948 | 1.0654 | 1.0785 | 1.072 | 1.0789 | 1.0886 | 1.0777 | 1.1051 | 1.1007 | 1.0964
Chart: Iteration
Width | 0.69042 | 0.14434 | 0.48188 | 0.69021 | 0.16071 | 0.94742 | 0.97384 | 0.40599 | 0.044109 | 0.75766 | 0.74539 | 0.86702 | 0.87246 | 0.61015 | 0.87725 | 0.90729 | 0.95158 | 0.98506 | 1 | 1
Start | 0.3004 | 0.9471 | 0.33895 | 0.81607 | 0.72937 | 0.77479 | 0.52736 | 0.17382 | 0.95025 | 0.24609 | 0.44565 | 0.43354 | 0.54084 | 0.38657 | 0.49877 | 0.51123 | 0.52988 | 0.54376 | 0.58779 | 0.65379
End | 0.18748 | 0.055084 | 0.29439 | 0.72382 | 0.055281 | 0.10863 | 0.087388 | 0.6211 | 0.067319 | 0.81426 | 0.14944 | 0 | 0.18974 | 0.20054 | 0.12306 | 0.11259 | 0.097498 | 0.087342 | 0.061726 | 0.032858
Angle | 0.22065 | 0.31689 | 0.49734 | 0.1195 | 0.022227 | 0.59275 | 0.61975 | 0.4664 | 0.24297 | 0.46054 | 0.59606 | 0.71928 | 0.54245 | 0.57329 | 0.6051 | 0.61169 | 0.62244 | 0.63139 | 0.66 | 0.69945
Offset | 0.2732 | 0.19839 | 0.82011 | 0.15025 | 0.22051 | 0.17214 | 0.81147 | 0.29851 | 0.8001 | 0.83787 | 0.8319 | 0.95273 | 0.75116 | 0.81767 | 0.81305 | 0.8128 | 0.81324 | 0.81455 | 0.82105 | 0.82959
(a) Tennis input
(b) Tennis output
Chart: Iteration
 | 0.44805 | 0.95026 | 0.60098 | 0.74329 | 0.69636 | 0.7868 | 0.78412 | 0.80757 | 0.7746 | 0.70353 | 0.771 | 0.89222 | 0.58037 | 1.2984 | 0.92848 | 1.6082 | 1.4938 | 1.5574 | 1.3935 | 1.609
Chart: Iteration
 | 0.69042 | 0.14434 | 0.48188 | 0.69021 | 0.16071 | 0.94742 | 0.97384 | 0.40599 | 0.044109 | 0.75766 | 0.14431 | 0.044366 | 0.15573 | 0.88251 | 0.24079 | 0.32063 | 0.40017 | 0.35996 | 0.34021 | 0.35501
 | 0.3004 | 0.9471 | 0.33895 | 0.81607 | 0.72937 | 0.77479 | 0.52736 | 0.17382 | 0.95025 | 0.24609 | 0.94943 | 0.94861 | 0.95254 | 0.83325 | 0.98937 | 0.50502 | 0.52388 | 0.51975 | 0.51866 | 0.51257
 | 0.18748 | 0.055084 | 0.29439 | 0.72382 | 0.055281 | 0.10863 | 0.087388 | 0.6211 | 0.067319 | 0.81426 | 0.059849 | 0.068128 | 0.11663 | 0.042291 | 0.072111 | 0.61165 | 0.46466 | 0.53655 | 0.57086 | 0.54915
 | 0.22065 | 0.31689 | 0.49734 | 0.1195 | 0.022227 | 0.59275 | 0.61975 | 0.4664 | 0.24297 | 0.46054 | 0.31144 | 0.24565 | 0.35295 | 0.65537 | 0.27324 | 0.72632 | 0.64283 | 0.68785 | 0.7107 | 0.6891
 | 0.2732 | 0.19839 | 0.82011 | 0.15025 | 0.22051 | 0.17214 | 0.81147 | 0.29851 | 0.8001 | 0.83787 | 0.20908 | 0.80073 | 0.085681 | 0.19566 | 0.14943 | 0.3557 | 0.42987 | 0.3929 | 0.37634 | 0.38303
(c) 3 motions input
(d) 3 motions output
Chart: Iteration
 | 0.69042 | 0.35009 | 0.92975 | 0.87569 | 0.34324 | 0.32681 | 0.3126 | 0.19779 | 0.3586 | 0.16594 | 0.025537 | 0.21771 | 0.15044 | 0.18288 | 0.235 | 0.20657 | 0.20842 | 0.18137 | 0.17705 | 0.146
 | 0.3004 | 0.14637 | 0.83828 | 0.57546 | 0.15218 | 0.16611 | 0.070166 | 0 | 0.017792 | 0 | 0 | 0.0093446 | 0 | 0 | 0 | 0 | 0 | 0 | 0.03665 | 0
 | 0.18748 | 0.54646 | 0.90524 | 0.75536 | 0.55661 | 0.58093 | 0.56334 | 0.49988 | 0.65768 | 0.66173 | 0.87732 | 0.58905 | 0.68763 | 0.70937 | 0.72662 | 0.75132 | 0.72034 | 0.70199 | 0.70155 | 0.69389
 | 0.22065 | 0.44821 | 0.096285 | 0.16254 | 0.44166 | 0.42596 | 0.54595 | 0.7318 | 0.49201 | 0.40003 | 0.36278 | 0.42016 | 0.39153 | 0.41666 | 0.42525 | 0.46395 | 0.36424 | 0.44855 | 0.46988 | 0.4615
 | 0.2732 | 0.21876 | 0.37787 | 0.8237 | 0.2078 | 0.18152 | 0.27474 | 0.21982 | 0.38638 | 0.49265 | 0.5755 | 0.44759 | 0.51465 | 0.48203 | 0.5085 | 0.43001 | 0.47538 | 0.50676 | 0.52059 | 0.49148
Chart: Iteration
 | 0.44805 | 0.90037 | 0.82681 | 0.47062 | 0.97183 | 0.86788 | 0.99163 | 0.7915 | 1.0247 | 1.1167 | 0.82349 | 0.66815 | 1.102 | 1.2072 | 1.1426 | 0.97554 | 0.74833 | 1.3444 | 1.1711 | 1.6464
Chart: Iteration
 | 0.69042 | 0.026876 | 0.46486 | 0.98123 | 1 | 0.26279 | 0.098306 | 0.062613 | 0.015521 | 0.92793 | 0.33801 | 0.068065 | 0.17651 | 0.35233 | 0.29324 | 0.39546 | 0.42853 | 0.77298 | 0.0063407 | 0.023943 | 0 | 0
 | 0.3004 | 0.57949 | 0.4204 | 0.95537 | 1 | 0.90287 | 0.2277 | 0.62049 | 0.45805 | 0.57746 | 0.93701 | 0.62674 | 0.50613 | 0.048134 | 0.66151 | 0.38384 | 0.43632 | 0.31394 | 0.93992 | 0.98298 | 1 | 1
 | 0.18748 | 0.45664 | 0.014986 | 0.65851 | 0.83842 | 0.8519 | 0.14099 | 0.36913 | 0.40142 | 0.40562 | 0.78179 | 0.35576 | 0.4158 | 0.63931 | 0.46088 | 0.6401 | 0.6247 | 0.82556 | 0.9741 | 0.99404 | 1 | 1
 | 0.22065 | 0.90961 | 0.25766 | 0.62724 | 0.73949 | 0.605 | 0.53927 | 0.86746 | 0.12172 | 0.81116 | 0.52728 | 0.86104 | 0.625 | 0.34103 | 0.029137 | 0.80862 | 0.81246 | 0.065257 | 0.9633 | 0.93417 | 1 | 1
 | 0.2732 | 0.46389 | 0.59568 | 0.39784 | 0.35356 | 0.47426 | 0.83556 | 0.33956 | 0.76699 | 0.21501 | 0.5049 | 0.32054 | 0.35741 | 0.40435 | 0.57547 | 0.61364 | 0.55236 | 0.84098 | 0.32615 | 0.3458 | 0.326 | 0.282
Chart: Iteration
 | 1.0479 | 1.0577 | 1.038 | 1.0876 | 1.0478 | 1.0699 | 1.0385 | 1.1077 | 1.0489 | 1.0526 | 1.1025 | 1.0593 | 1.0609 | 1.0614 | 1.0749 | 1.0876 | 1.0709 | 1.0763 | 1.1129 | 1.1087 | 1.1023 | 1.1093